## Slide 1: Coupling FEM and atomistic models for electronic device simulations: The TiberCAD approach
Alessandro Pecchia
University of Roma “Tor Vergata”
M. Auf der Maur, G. Penazzi, F. Sacconi, G. Romano
A Gagliardi, F. Santoni, A. Di Carlo
CNR - ISMN Institute for Nanostructured Materials

## Slide 2
Tiber…

## Slide 3: TiberCAD people
Prof. Aldo Di Carlo
Dr. A. Pecchia
Dr. G. Romano
Dr. A. Gagliardi
Dr. M. Auf der Maur
Dr. F. Sacconi
Dr. G. Penazzi
Multiscale Device Simulator
http://www.tibercad.org
Mr. F. Santoni
Mr. W. Rodrigues

## Slide 4
DSSC/OPV module
Applications
Charge transport in organic semiconductors
Memristors
Inorganic LED (InGaN)
Quantum DOTs
1 nm
Contact
Tunnel distance
300 nm
Nanofilaments
Piezoelectricity
Heat dissipation

## Slide 5: multiscale/multiphysics
Package Level
Poisson/Drift Diffusion
QM regions
Strain
Device Level
Atomistic Level
Different physical models on different scales are needed to describe electronic devices

## Slide 6
1 A
1 nm
10 nm
100 nm
1 um
Features:
drift diffusion, strain, thermal, EFA
VFF, ETB, DFTB
Organics, DSSC modelling.
Introduction: TiberCAD

## Slide 7
Classical Regions
Elasticity
Drift-Diffusion
Quantum Regions
Env. Funct.(kp)
Valence FF
Empirical TB
DFTB
Atomistic

Finite Elements
Ec ,Ev

converse piezo
structure
elasticity
guess
2
Models overview
Thermal

## Slide 8: Multiscale/multiphysics schemes
DOMAIN 1
DOMAIN 2
BRIDGE METHOD
each domain provides boundary conditions to adjacent domains.
o
domain 2
domain 1
OVERLAP METHOD
each model computes physical quantities that act as parameters to the other models.
Schrödinger/Poisson
Transport parameters from DFT
NEGF/drift-diffusion
VFF/continuous elasticity
M. Auf der Maur, G. Penazzi , G. Romano, F. Sacconi, , A. Pecchia , A. Di Carlo
IEEE Trans. Electron Devices, 58, 1425 (2011)

## Slide 9
Overlap Multiscale
Schrodinger + Drift Diffusion

## Slide 10: Energy/Position Multiscale
Energy
Position
n-AlGaN
p-AlGaN
GaN
Active region
Min CB
Max VB
Quantum density: K.P
Quantum density: ETB
Classical density
Drift-Diffusion Transport

## Slide 11: Envelope Function Approx
In TiberCAD:
kp Hamiltonian generalizes single band dispersions
Envelope function
k is interpreted as the usual momentum operator:
Full Band kp
Cardona-Pollak (1966)
G. Fishman (2004)

## Slide 12: InAs Qdots
M. Buda et. al., IEEE Journal of Quantum Electronics, 2003

## Slide 13: InGaAs Quantum wire: overlap scheme
current crowding in the wire
quantum region
embracing
holes
electrons
Self-consistent densities at Vb = 1.3 V
cathode
anode
K.P quantum model
Notes: 13

## Slide 14
TiberCAD includes a technique for mixing classical and quantum density, acting as a quantum correction to drift-diffusion calculation
Embracing region where classical and quantum charge are mixed.
Embracing technique
The mixing parmeter is solution of a Laplace equation with Dirichelet boundary conditions 0.0 and 1.0

## Slide 15
Barrier and well embracing: Well is quantum + classical
Alternative: Quantum+Classical

## Slide 16
InP dots for gas sensing
Idealized dot
Realistic dot
Strain field maps
AFM image:
Closely coupled dots
D. Barettin et al. Nano (2014)
D. Barettin et al. J. Appl Phys (2015)

## Slide 17: Electronic properties
Electron states
Hole states

## Slide 18: Comparisons between dots
el:
hl:
el:
hl:
homo-nuclear dots
hetero-nuclear dots

## Slide 19: Shape and alloy effects in Qdot system
EBL
Qdots (islands)
TEM image (In comp.)
Imported alloy concentration
Strain profile
Constant In concentration


## Slide 20
Impact of lateral coupling given mainly by strain field (continuum and k*p 3D model): shift of the spectrum of the central dot of about 90meV
Lateral coupling via strain

## Slide 21
Hole current density
electron current density
Increasing electron current density with electron-rich layer
Current densities

## Slide 22
Quantum Transport: NEGF
Bridge Multiscale

## Slide 23
Classical Regions
Elasticity
Drift-Diffusion
Quantum Regions
Env. Funct.(kp)
Valence FF
Empirical TB
DFTB
Atomistic

Finite Elements
Ec ,Ev

converse piezo
structure
elasticity
guess
2
j
Models overview
NEGF
Thermal

## Slide 24: Open quantum systems
Effective Scattering Region
Left Lead
Right Lead

## Slide 25: libNEGF
libNEGF
phonons
Quantum-classical interfaces
Atomistic
Continuous
http://www.bitbucket.org

## Slide 26
N-1 dimensional Contacts
Automatic mesh creation using libMESH classes
General extrusion of planar contacts in 1,2,3D
NEGF: contact generation

## Slide 27: Example: MOS with NEGF
S
D
drift-diffusion
NEGF
Fully self-consistent
25 nm
Mix between overlap (Schrödinger/Poisson) and bridge (current at NEGF boundary) schemes

## Slide 28
NEGF: input file
In negf regions, solve only for electrostatic potential, (not for electron current)
S
D
Module negf{
regions = channel
Physics{
Hamiltonian efa {}
}
}
Module selfconsistent
{
solve = (negf, driftdiffusion)
Multiscale bridge {
macromodel = driftdiffusion
micromodel = negf
restrict_variables = (fermi_e)
}
max_iterations = 10
absolute_tolerance = 1e-3
relative_tolerance = 1e-9
}

## Slide 29: MOS: quantum/classical
z (um)
density
Vg = 0.1-0.7 V
x (um)

## Slide 30: RTD devices
RTD structure
0.2 V
0.5 V

## Slide 31: InGaN/GaN multi QW
injection
nonradiative losses
Trap-assisted tunneling
spontaneous emission
Peculiarities:
Strong built in field due to spontaneous and piezoelectric polarization (wurtzite crystal)
Large injection barriers
Deep acceptor donor level

## Slide 32: Motivation: why InGaN/GaN
Tunable gap across visible: high efficiency/efficacy LEDs
Theoretically could allow for all-nitride phosphor-free white light
Challenge: InN GaN are 10% lattice mismatched !
Kaun et al, Semicond. Sci. Technol. 28 074001,2013
VCA

## Slide 33: InGaN/GaN specific issues
InGaN/GaN QW LEDs suffer from two severe efficiency issues
The reasons are not well known yet: simulations as helpful tool
peak emission efficiency
Source: generalwafertechnology.com
  “green gap”:
   Efficiency droop:

## Slide 34: Example: excited states
Here we use NEGF to calculate the LDOS, on top of a DD simulation (no selfconsistency)
NEGF based LDOS give more insight into spatio-spectral features
«standard Schrödinger» approach is less efficient
Future:
Photogeneration from el-g coupling will allow to asses importance of leakage in PL experiment
2 nm QWs
4 nm QWs
Energy
position
2 nm QW
4 nm QW

## Slide 35: Difficulties
Difficulties: separate n/p densities near equilibrium
Below knee voltage the minority carrier densities become extremely low
Reproduce non-radiative recombinations in NEGF (Auger, SRH)
Introduce el- coupling in NEGF
Energy
Position (nm)
Log(occupation)
work in progress

## Slide 36: Importance of non-radiative losses
Forward current at low injection, for different devices (different QW thickness, different In content)
Correlation between fitting parameters and independent mechanical data

## Slide 37
nm
m
mm
Quantum Devices
Atomistic
Semi-Empirical
Atomistic
Ab-initio
ms
s
ps
ns
Tiume scale
Coupling atoms with finite elements
Classical transport
Finite Elements

## Slide 38: Atomistic structure generation
We can assure a consistent atomistic structure using a top down approach:
1. Identify relevant volume
2. Shift origin slightly inside
3. Fill up with atoms using the crystal basis
4. Cut atoms outside of the structure
It is important that all atoms are lying inside the simulation domain
Dr


we assume pseudomorphic structures with commensurate interfaces

## Slide 39: Valence Force Field
We included a Keating model to calculate strain at an atomistic level
The equilibrium position is that one which minimizes U
We use a nonlinear conjugate gradient minimization technique
Keating (1966) D. Camacho, Y. M. Niquet (2009) Penazzi Gabriele, PhD. Thesis (2010)

## Slide 40: VFF vs Elasticity
Evaluating when Continuum Elasticity failures is not trivial.
It depends on structure geometry. In general, it fails near interfaces
InAs quantum dot on GaAs substrate
Self assembled by strain relaxation
High lattice mismatch (about 7%)
15% differences

## Slide 41: VFF vs Elasticity II
Increase height up to 5 nm
Smaller differences on low aspect/ratio structures
VFF is fundamental also to include internal strain here!

## Slide 42: Empirical Tight Binding
Y
Cia
f= orbital
matrix notation:
HC=EC

## Slide 43: Empirical Tight-Binding
The sp3s* Hamiltonian [Vogl et al. J. Phys. Chem Sol. 44, 365 (1983)]
The sp3d5s* Hamiltonian [Jancu et al. PRB 57 (1998); PRB (2001)]
GaN

## Slide 44
Alloys

## Slide 45: Alloys
Can treat alloys in two ways: VCA (virtual crystal approximation, effective material) or ‘real’ structure (e.g. random alloy)
  In VCA matrix elements are taken as mean values:
    InxGa1-xN = x*(InN) + (1-x)*(GaN)
  otherwise onsite elements according to the atom and hopping element according to the pair
In
In
Ga
Ga
N
InGa
InGa
InGa
InGa
N
VCA:
‘real’:
requires supercell + statistical ensemble
Note: we like parameter sets where the common atom (N) is consistent between InN and GaN

## Slide 46: Modelling nanopillars
small footprint on the substrate, allows:
defect-free material
growth on various substrates (Silicon)
growth on large area substrates without lattice strain
Empirical Tight binding model sp3d5s*+SO
Solve few states using Lanczos
M. Auf der Maur IEEE TED (2011)

## Slide 47: InGaN nanocolumns
2.117nm
2.071nm
2.073nm
|---9.464nm---|
51714 Atoms Strained + VFF x(In=0.10).xyz
GaN
InGaN
GaN

## Slide 48: InGaN nanocolumns
2.159nm
2.066nm
2.073nm
|---9.534nm---|
51714 Atoms Strained + VFF x(In=0.20).xyz
GaN
InGaN
GaN

## Slide 49: InGaN nanocolumns
2.221nm
2.061nm
2.074nm
|---9.653nm---|
51714 Atoms Strained + VFF x(In=0.35).xyz
GaN
InGaN
GaN

## Slide 50
  VCA
  Random uniform
  Random with clustering
2 nm
14 nm
10 nm
InGaN
GaN
GaN
GaN
Uniform distribution is first applied to the structure (e.g. 70% uniform and 30% clustering)
Probability of Substitution of a Ga atom in GaN with In is higher if other In atoms are already in a sphere of 1nm radius around the atom.
Modelling nanopillars

## Slide 51
30% clustering
No clustering
Modelling nanopillars

## Slide 52
el
hl
el
hl
30% clustering
No clustering
ETB groundstates

## Slide 53
xx strain from elasticity macroscopic model (VCA)
VFF on a VCA structure
VFF on a random sample
xy plane in the InGaN region
VFF and elasticity models

## Slide 54
Strain from VFF on a random sample
uniform distribution
clustering
Effects of clustering

## Slide 55
In 10%
In 30%
FWHM = 35 meV
FWHM = 18 meV
Optical Spectrum – no clustering

## Slide 56
Distribution of energy gaps
Mean = 3.329
Std = 0.0278
skew = -1.242
Distribution of energy gaps
Mean = 2.793
Std = 0.028
skew = -0.708
In 10%
In 30%
FWHM = 45 meV broadening
FWHM = 20 meV broadening
Optical Spectrum – 30% clustering

## Slide 57
  Clustering effect:
  Larger spread in random distribution
  Lowering of mean Et
Correlation between ground state transition energy and optical strength
Increasing spread in random distribution with higher x(In)
VCA overestimates Et and Opt.strength

## Slide 58: Localization behavior in InGaN QW
Correlation of local In concentration with wave function localization
Electrons and holes subject to different In fluctuations planes
min. |M|
max. |M|
el, hl

## Slide 59: Effect of non-uniformity
Local In concentration
counts
Theory for uniform alloy
uniform
70% uniform
40% uniform
QW:
Environment dependent substitution probability

## Slide 60: InGaN QW: optical matrix element
Lateral localization leads to strong fluctuations in optical matrix elements
25% In
Fluctuation both in energy and M, icreasing with In concentration
Correlation between Eg and MME
Increasing deviation from VCA values

## Slide 61: CUDA developments
Lambda state
1,000,000 atoms on a WS!
W. Rodrigues, A. Pecchia, A Di Carlo, Comp. Phys. Comm. (2014)

## Slide 62
Software Development ToolKit

## Slide 63
Software Development toolKit
 Allows to add new modules by user without relinking core
Module somename
{
Physics {
mobility constant { }
}
}
library name mobility_constant.so
library name somename.so
TiberModelObject
PhysicalModelInterface
PhysicalObject
SimulationInterface
Handles instantiation from shared libraries, option container, basic functionality
Physics {
mobility constant { }
}
Module driftdiffusion
{
}
Base class of all physical entities
bulk, interface, edge, node

## Slide 64
Module poisson {
Physics {
charge_density constant {
}
}
}
#include "SimulationInterface.h"
class Poisson : public SimulationInterface
{
public:
static Poisson* create(options);
protected:
virtual void do_init(void);
virtual void parse_options(void);
virtual void do_setup_solution_variables(void);
virtual void do_solve(void);
virtual PhysicalModel* create_bulk_model(options, material);
virtual PhysicalModel* create_boundary_model(options, boundary);
virtual void get_solution_secure(element, data, points);
private:
};
Example: Poisson

## Slide 65
Conclusions
Multiscale/multiphysics is requested for simulation of real modern electronic devices where electronics, optics, chemistry are linked together
We have seen the most important physical models implemented in tiberCAD
We have discussed the basics of how to couple atomistic and classical simulations
Much effort is still needed to arrive at a true multiscale integration for transport simulations
Additional info about TiberCAD: http://www.tibercad.org
info@tiberlab.com
www.tiberlab.com
Download free trial version:

## Slide 66
THANK YOU !

## Slide 67: Transport across EBL
tunneling across Al0.2Ga0.8N EBL:
Considerable fluctuations due to random alloy: similar to defect assisted tunneling
RND
<RND>
VCA

## Slide 68: Inter-well transport in LED
tunneling across In0.05Ga0.95N barrier:
Extracted barrier resistivity:
Pure drift-diffusion: 15 Wcm2
8 band kp: 1.33 Wcm2
Random alloy: 0.28 – 1.26 Wcm2
 More realistic ON current:

## Slide 69: Oxide-tunneling
Coupling DD with
balistic tunneling,
quantum density
Sacconi et al IEEE TED 2004 and 2007
M. Auf der Maur et al. J. Comp. Elect., 7 398 (2008)
-critobalite
tridimite
-quartz

## Slide 70: Bridge method: flux continuity
G
D
S
Y
G
D
S
X
Y
Poisson-Drift-Diffusion is solved in the whole device
Tunneling current calculated with atomistic tight-binding model is taken as a boundary condition for electron continuity at Si/oxide interface
Self consistent cycle
JC,V(x,y)
JC(l) = JQ(l)
l
l
JC,V(x,y)
X
Notes: 70
Let’s consider an example fitting to the first case.
Here we have a MOS, source, drain and gate. Here we have the oxyde. The oxyde, treated classically is a ideal electrical insulating but we know that quantistically not. We know that across this junction flows the tunnelling current. One could think to adopt a quantum-mechanically approach everywhere but the computational cost becomes too large. The idea is, therefore, using two different approach for each domain.
And what do it happen along this interface? Our idea is imposing the continuity of the density current.
Let’s briefly see the proposed algorithm which accomodates this condition.
Let’s assume a local coordinate landa in this way. We assume that, at the first step the quantum current is zero. We solve the drift diffusion simulation which gives the electrostatic potential turned out along the oxide interface. This potential is the boundary condition for the quantum
simulation which in own turn computes the quantum current through some quantum transport simulation (Empirical Tight Bindind, Density Functional Method or whatever). This current becomes the new boudnary condition for the drift diffusion simulation and so on.
70