## Slide 1: Coupling FEM and atomistic models for electronic device simulations: The TiberCAD approach
Alessandro Pecchia
University of Roma “Tor Vergata”
M. Auf der Maur, G. Penazzi, F. Sacconi, G. Romano
A Gagliardi, F. Santoni, A. Di Carlo
CNR - ISMN Institute for Nanostructured Materials

## Slide 2: TiberCAD people
Prof. Aldo Di Carlo
Dr. A. Pecchia
Dr. G. Romano
Dr. A. Gagliardi
Dr. M. Auf der Maur
Dr. F. Sacconi
Dr. G. Penazzi
Multiscale Device Simulator
http://www.tibercad.org
Mr. F. Santoni
Mr. W. Rodrigues

## Slide 3
DSSC/OPV module
Applications
Charge transport in organic semiconductors
Memristors
Inorganic LED (InGaN)
Quantum DOTs
1 nm
Contact
Tunnel distance
300 nm
Nanofilaments
Piezoelectricity
Heat dissipation

## Slide 4
Organic transport in TiberCAD

## Slide 5: Organic devices
Challenge:
Interface problem
Local electric field
Morphology
Schottky

## Slide 6: Model basics
Electron energy barrier
Hole energy barrier
  Bulk model
Injection models
Drift-Diffusion Model
Thermionic Injection
Thermionic Injection
F. Santoni, A. Gagliardi, M. auf der Maur, A. Di Carlo, Organic Electronics 15 (2014) 1557–1570
Notes: Qui mettere un breve riassunto di come modelliamo la cosa

## Slide 7: Injection Model
J.C. Scott, G.C. Malliaras, Chem. Phys.Lett. 299 (1999) 115.
C.R. Crowell, S.M. Sze, Solid State Electron. 9 (1966) 1035.
Current boundary condition:
n0 p0 equilibrium densities
Scott-Malliaras model for charge injection
Longevin recombination with image

## Slide 8: Field dependence
g(f)

## Slide 9: Mobility model
Mobility is dependent on carrier density n and electric field F
n
F
n
n
Mobility is strongly dependent on the energy disorder parameter s
W. F. Pasveer et al., Phys. Rev. Lett. 94 (2005) 206601

## Slide 10: Induced Density of Interfacial States
The IDIS model applies when contact/organic chemical interactions are moderate but non-negligible
DOS at the interface may originate from trap states or Metal-induced states (MIGS)
A.M. Cowley, S.M. Sze, J. Appl. Phys. 36 (1965) 3212.
The charge neutrality level is like the
Fermi level of the organic at the interface
Assume constant gap DOS at the interface
Vasquez, Flores, Kahn, Org. Elect. 8 (2007) 241

## Slide 11
LUMO
HOMO
CNL
+
-
LUMO
HOMO
CNL
+
-
Dipole shift
Self-consistent equation:

## Slide 12: Determination of parameters
LUMO
HOMO
CNL
+
-

## Slide 13
Referred to HOMO
S and b can be determined experimentally fitting different metal WF.

## Slide 14: Determination of parameters
S and b can be determined experimentally.
Referred to HOMO

## Slide 15: ITO/CuPc/α-NPD/Alq3/LiF/Al

## Slide 16: Importance of interfaces
ITO
Al
Alq3
ITO/Alq3/Al
Fitting mobility model alone is not enough.
I-V characteristics are determined also by the level alignment.
?

## Slide 17: Trap-assisted tunneling
Gap dos can explain low bias current

## Slide 18: P3HT/TiO2 morphology
=
=
Paul A. Midgley & Rafal E. Dunin-Borkowski , “Electron tomography and holography in materials science”, Nature Materials 8, 271 - 280 (2009) .

## Slide 19: Model of the blend
3 μm
Anode
Eff. Material
Eff. Material
Eff.
Material
Eff.
Material
Buffer
(Eff. Mat.)
20 nm
Real Morphology
180 nm
Buffer
(Eff. Mat.)
20 nm
Light
TiO2
HTM

## Slide 20: Effect of interface traps
No interface traps
Interface traps
Electric field intensity (V/cm)

## Slide 21: Effect of traps II
No traps
Traps at the interface

## Slide 22: Effective model
Effective (low mesh)
Effective (low mesh)
Photoanode
Cathode
DOS renormalization
R and G renormalization

## Slide 23
Conclusions
Multiscale/multiphysics is requested for simulation of real modern electronic devices where electronics, optics, chemistry are linked together
We have seen the most important physical models implemented in tiberCAD
We have discussed the basics of how to couple atomistic and classical simulations
Much effort is still needed to arrive at a true multiscale integration for transport simulations
Additional info about TiberCAD: http://www.tibercad.org
info@tiberlab.com
www.tiberlab.com
Download free trial version:

## Slide 24
ELBE LAB ?
THANK YOU !